## Slide 1: BUILDING MATERIALS

## Slide 2
Activity concentration in building materials
Reference levels
Controls
Content

## Slide 3
Natural Radioactivity of Building Materials
All building materials contain various amounts of natural radioactive nuclides.
Materials derived from rock and soil contain mainly natural radionuclides of the U and Th series, and the radioactive isotopes of potassium (K-40)
In the U series, the decay chain segment starting from radium (Ra-226) is radiologically the most important and therefore reference is often made to radium instead of uranium
Worldwide average concentrations in the earth’s crust
  radium: 40 Bq/kg, thorium: 40 Bq/kg, potassium: 400 Bq/kg

## Slide 4
Activity Concentration in Building Materials
Material | Typical activity concentration (Bq/kg) |  |  | Maximum activity concentration (Bq/kg) |  | 
Most common buildings | 226Ra | 232Th | 40K | 226Ra | 232Th | 40K
Concrete | 40 | 30 | 400 | 240 | 190 | 1600
Aerated and light-weight concrete | 60 | 40 | 430 | 2600 | 190 | 1600
Clay (red) bricks | 50 | 50 | 670 | 200 | 200 | 2000
Sand-lime bricks | 10 | 10 | 330 | 25 | 30 | 700
Natural building stones | 60 | 60 | 640 | 500 | 310 | 4000
Natural gypsum | 10 | 10 | 80 | 70 | 100 | 200
Most common industrial by-products used in building materials |  |  |  |  |  | 
By-product gypsum (phosphogypsum) | 390 | 20 | 60 | 1100 | 160 | 300
Blast furnace slag | 270 | 70 | 240 | 2100 | 340 | 1000
Coal fly ash | 180 | 100 | 650 | 1100 | 300 | 1500

## Slide 5
Reference Level for Building Materials
Reference level of “annual effective dose to the representative person generally that does not to exceed a value of about 1 mSv” (para. 5.22)
Several countries restrict the amount of radionuclides of natural origin in building materials
Safety Guide SSG-32 proposes the use of an activity concentration index as a screening tool for identifying building materials that may need to be subject to restrictions

## Slide 6
Reference Level for Building Materials
is activity concentration of 226Ra, :232Th, :40K
I < 1 for bulk materials or I < 6 for superficial materials (e.g. tiles), then annual effective dose less than reference level of 1 mSv
The activity concentration index should be used only as a screening tool for identifying materials which might be of concern.
Any actual decision on restricting the use of a material should be based on a separate dose assessment.
Such assessment should be based on scenarios where the material is used in a typical way for the type of material in question.
Scenarios resulting in theoretical, most unlikely maximum doses, should be avoided.

## Slide 7
Flow-chart of the recommended system of control of building materials
Determine activity concentration of radionuclides in the building materials
Determine activity index
No restrictions
Assess dose
No restrictions
Decide on appropriate
measures
E<reference level = 1mSv
E>reference level = 1mSv
I1 (or 6)
I1 (or 6)

## Slide 8
Gamma Radiation from building materials in existing building
Protective actions may be necessary for existing buildings with high annual effective dose levels caused by gamma radiation due to radionuclides in the building materials.
If considered necessary, the national authority should establish reference levels for exposure to gamma radiation emitted from building materials in existing buildings.
  Feasible protective measures are not easy to implement.
Note that the protective measure carries serious economic and penalties and should not be applied without careful consideration.

## Slide 9
Key Message
Some NORM residues are used as building materials
National responsibility to set a reference level
Controls may be necessary