## Slide 1: Management of Bulk NORM Residues and Waste (Part 2)

## Slide 2
Content
Scale
Sediments and sludges
Slag
Furnace dust
Liquid residues
Gaseous residues
Monitoring and Surveillance
Public doses from NORM facilities
References

## Slide 3
Scale
Scale containing elevated activity concentrations forms inside pipes, valves, pumps, vessels and filtration systems
Process | Radionuclide | Activity concentration (Bq/g)
Oil and gas production | 226Ra | 0.1 – 15 000
Phosphoric acid production | 226Ra | 0.03 – 4000
Titanium dioxide pigment production | 226Ra | <1 – 1600
Chemical processing of zircon | 226Ra | >5000
Coal fired steam generation | 210Pb | Can exceed 100
Coal mining, Ra-rich inflow water | 226Ra, 228Ra | Up to 200
Notes: Scale can occur anywhere – where you use natural materials and pH and temperature change.

## Slide 4
Scale
Pipe scale in a phosphoric acid plant
Photographic image
SEM image

## Slide 5
Scale
Oil and gas production ‘tubulars’
After scale removal
Before scale removal

## Slide 6
Scale
In most NORM scale, 226Ra is the predominant radionuclide
  Sometimes 228Ra from the 232Th decay series as well
Some scale may contain elevated levels of 210Pb
The presence of high activity concentrations may require special radiation protection precautions when equipment is opened for maintenance
Scale may be difficult to remove, and various methods need to be considered:
  Mechanical, e.g. boring, reaming
  Chemical
  Abrasive, including high pressure water jetting
  Melting as scrap

## Slide 7
Scale removal
Scale removal may itself create radiological hazards to workers
Scale removal creates NORM waste in solid or liquid form
  This waste has to be disposed of in an acceptable manner
Outside companies performing decontamination or scrap melting may have to be authorized by the regulatory body

## Slide 8
Scale removal in oil and gas production
Scale removal using high pressure water jet
Dry drilling of tubulars with closed extractor system

## Slide 9
Melting facility for NORM contaminated scarp
The radionuclides migrate to the slag, leaving the steel free of radioactivity
Mixing with larger amounts of non-contaminated scrap can reduce activity concentrations and exposures to levels below radiological concern

## Slide 10
Options for management of scale after removal
Reintroduction to the process to recover residual minerals of value
Burial at the site (where the site will be under institutional control after closure – e.g. mine sites)
Disposal at a hazardous waste disposal facility
Disposal at a low/intermediate level radioactive waste facility
Indefinite storage in drums at controlled storage facilities
The oil and gas industry has some additional options:
  Discharge from offshore rigs into marine waters
  Injection into well field formations
  Disposal in abandoned wells
In all cases, an appropriate risk assessment is necessary

## Slide 11
Sediments and sludges
Process | Radionuclide | Activity concentration (Bq/g)
Rare earth extraction | 228Ra | 0.6 – 10 000
Oil and gas production | 226Ra | 0.05 – 800
Niobium extraction | 226Ra, 228Ra | 200 – 500
Zircon chlorination | 226Ra | 0.3 – 48
Titanium dioxide pigment production | 232Th | 0.02 – 24
Iron smelting | 210Pb | 12 – 100
Water treatment | 226Ra | 0.1 – 14
Phosphate fertilizer production | 226Ra | 1.3 – 4.3

## Slide 12
Sediments and sludges
Activity concentrations vary over a wide range
Depending on the activity concentration, some sediments and sludges have to be treated in a similar manner to high activity scale
  In many cases, engineered shallow ground burial in earthen trenches or concrete silos is the preferred option
Lower activity sediments and sludges (of the order of 10 Bq/g or less) are generally suitable for disposal at normal industrial waste or hazardous waste facilities

## Slide 13
Slag
Process | Radionuclide | Activity concentration (Bq/g)
Niobium extraction from pyrochlore | 232Th | 20 – 120
Tin smelting | 232Th | 0.07 – 15
Copper smelting | 226Ra | 0.4 – 2
Thermal phosphorus production | 238U | 1

## Slide 14
Slag
There are many opportunities for using slag as a by-product ;
  as a construction material (or component of construction material)
  Resource for extraction of contained metals
Slag with higher activity (from steel, niobium, tin, copper etc. production) may need to be restricted
  A detailed assessment is necessary
Slag with lower activity concentration, e.g. thermal phosphorus slag, can be used in the construction of roads, dams, etc.
  Its use in house construction may need to be subject to certain conditions

## Slide 15
Furnace dust
Process | Radionuclide | Activity concentration (Bq/g)
Extraction of niobium from pyrochlore | 210Pb, 210Pb | 100 – 500
Fusion of zircon | 210Po | 600
Thermal phosphorus production | 210Pb | 1,000
Tin smelting | 210Pb, 210Pb | Up to 200

## Slide 16
Furnace dust
Furnace dusts contain volatile radionuclides (lead and polonium)
Can have high activity concentrations
Usually requires disposal in a regulated facility
Consider worker exposure during scrubber and incinerator maintenance (or where dusts may accumulate)

## Slide 17
Liquid residues
Can involve large volumes (e.g.; Mine water)
Excess water from tailings dams, phosphogypsum stacks, etc.
Recirculated process water and contaminated rainwater
Used process water streams:
  Water separated from slurry streams
  Wash water
  Flotation water
  Spent leach solutions
  Gas scrubbing water
Water from decontamination of equipment
Spent solvents
‘Produced water’ from oil and gas production
  Formation water and injection water

## Slide 18
Liquid residues-management options
Recycle to the process
  By far the most widely used option
  Can be used for aqueous residues and spent solvents
Treatment + discharge
  Neutralization — neutralizing agents, mixing acidic & alkaline streams
  Settling, precipitation, filtration — can remove up to 90% of 226Ra etc.
  Treatment for compliance with (non-radiological) effluent treatment standards in terms of environmental regulation is usually adequate also for radionuclides
  Treatment generates solid waste (sludge, filter cake)
Evaporation and seepage ponds
  Subsequent land remediation and management of solid waste
Slurry with sand and return to mining void
Direct discharge to large water bodies, e.g. marine waters

## Slide 19
Liquid residues – oil and gas
Management options for ‘produced water’ from oil and gas extraction:
  Can be generated in very large volumes
    Oilfields: 2400 – 40 000 m3/day
    Gas fields: 1.5 – 30 m3/day
  Wide range of activity concentrations
    0.002 – 1200 Bq/L 226Ra
  Options:
    Discharge to marine waters (mainly for offshore facilities)
    Reinject into reservoir
    Pump to seepage/evaporation ponds
      Subsequent land rehabilitation and disposal of solid waste

## Slide 20
Gaseous emission
Gaseous emissions arise from furnaces, chemical processes and ventilation systems
Sources of exposure:
  U and/or Th series radionuclides in airborne dust particles
  Radon
Emission standards in terms of environmental regulation:
  Reduced emission of hazardous constituents, including radionuclides
  Improved atmospheric dispersion, e.g. stack height
Emission controls:
  Dust filters and precipitators
  Gas scrubbers
Emission control generates solid and liquid NORM residues:
  Captured dust particles
  Scrubber liquids — water, NaOH

## Slide 21
Monitoring and surveillance
The facility operator is responsible for the design and implementation of a suitable monitoring and surveillance programme
Monitoring:
  Monitoring of discharges
  Monitoring of materials and equipment before removal from the facility for scrap or repair
  Environmental monitoring
Surveillance:
  Physical inspection to verify the integrity of waste management systems including structures and components
Notes: Pllies to both BULK and smaller volumes of waste/residues

## Slide 22
Discharge monitoring
The purpose of discharge monitoring is to verify that the amounts of activity being discharged are within the discharge limits established for the facility
  This in turn helps to ensure that the optimization process is being implemented as intended and that doses received by members of the public are within the dose limit
All liquid and gaseous discharges, including entrained dust particles, should be monitored

## Slide 23
Monitoring residual materials/
equipment prior to removal from site
For purposes of clearance (removal from regulatory control), monitoring is necessary for verifying compliance with NORM clearance criteria:
For removal from the site for disposal, recycling or repair, monitoring is necessary for:
  Verifying compliance with the Transport Regulations, where applicable
  Verifying compliance with the acceptance criteria of the receiving facility
Notes:   clearance criteria:
    Mass activity concentration 1 Bq/g (U, Th series), 10 Bq/g (40K)
    Surface activity concentration such that the annual dose does not exceed 1 mSv

## Slide 24
Environmental monitoring
The purpose of environmental monitoring is:
  To evaluate the effectiveness of the waste management control measures
  To assess doses received by members of the public
  To assess the environmental impacts
Environmental regulation will also require the monitoring of non-radiological components
Monitoring programme:
  Frequency
  Environmental media to be considered:
  Radionuclides to be considered
Notes: Refer to later lecture on environmental monitoring

## Slide 25
Potential Disposal Options
Disposal alternatives for NORM wastes. Disposal of more concentrated wastes requires greater isolation of waste from the general public (from IAEA TRS49)

## Slide 26
Public doses from NORM facilities
Annual dose to the representative person (μSv):
  Uranium tailings, Germany: <1000
  Uranium tailings, Brazil: 350
  Uranium residues, Romania: 51
  Gold mine tailings, South Africa: 30 (1.5 – 140)
  Mining and beneficiation of rare earth ores: 0 – 44
  Extraction and purification of rare earths: 0 – 30
  Zircon and zirconia production: 0.01 – 37
  Mining and beneficiation of phosphate rock: <10 – 27
  Phosphoric acid production: Trivial
  Phosphate fertilizer production: 0 – 4
  Phosphate animal feed production: 11 – 30
  Thermal phosphorus production: 1
  Titanium dioxide pigment production: Trivial

## Slide 27
Key messages
Doses arising from solid, liquid and gaseous NORM residues are generally very low
Small to moderate quantities of solids with higher activity concentrations
Larger volumes of liquids
Can be regarded as potential resources
Appropriate protection is achievable through different management options